Workshop Molecular Photoreactivity on Metal-Oxide Surfaces from First-Principles

Madrid 4th – 5th December 2009

Reactivity and Chemical Reactions of Faceted TiO2 Nanoparticles

James P. Lewis

West Virginia University, Department of Physics, Morgantown, WV 26506-6315, USA				email: james.lewis@mail.wvu.edu

Abstract

Although anatase is a less stable crystallographic phase than rutile in bulk titanium dioxide materials, it has received considerable attention in photoactive materials related applications due to increased high reactivity in the anatase polymorph (1, 2). More interestingly, it is reported that anatase, instead of rutile, becomes the preferable stable phase for TiO2 for particle sizes less than 14nm (3, 4). Therefore, an important step in achieving a full understanding of anatase nanoparticles’ photoactive functions with regards to their surface’ characteristics is to examine and determine specific active sites that are available for probing molecules surface adsorption and dissociation.

In previous reported work, the (101) surface is found to be the majority surface dominating the exposed shape on nanosized anatase crystallites (3, 4, 7-9). However, the minority surfaces (001) are the most reactive for photocatalytic reactions on anatase surfaces (10-16). In this work, we attempt to understand the relationship between the unique electronic properties and surfaces of anatase nanoparticles by investigating faceted nanoparticles which have both the (001) and (101) surfaces in different percentages. A critical question is where active sites are located in relation to this intersection. In this work, we aim to address this question by theoretically investigating specially constructed anatase nanoparticles with co-existing (101) and (001) surfaces and predict where the active sites and potential adsorption and dissociation will most likely occur.

There are obviously structural changes appearing in the surface areas in the nanoparticles; the most noted structural changes occur at the edged Ti atoms which are connected between (001) facets and (101) facets. One nanoparticle (182 atoms) is shown in Fig. 1 (a) as an example which demonstrates the exact locations of edged Ti atoms in the initial structures before optimization. As a result of optimization, the edged Ti atoms move outward which results in extended Ti-O bonds; these edged Ti atoms are lower coordinated in the optimized structures. The primary result is that the edged Ti atoms connected between the (001) and the (101) surfaces exhibit the most significant structural changes; the original four-coordinated Ti atoms become three-coordinated which make them very reactive sites exposed at these surfaces.

(a)       (b)

Figure 1. An example of a faceted anatase nanoparticle; the edged Ti atoms are labeled yellow which are 3- or 4-coordinated Ti atoms connected between (001) and (101) surfaces. The PDOS (projected density of states) is also displayed. The red plots represent states from Ti atoms and black plots from O atoms in nanoparticles. The peak mid-gap corresponds to the lower-coordinated Ti corner atoms.

A further analysis of the electronic structures provide a complete understanding of the relationship between these low-coordinated edged Ti atoms and the reactive properties. The density of states for the 182 atom nanoparticle system is shown in Fig. 1(b). The energy gap of our model nanoparticles are approximately 3.5 eV which are larger than bulk’s band gap. A feature in the PDOS plots indicates the existence of mid-gap frontier orbitals. These small peak states occur near the Fermi energy, which is approximately 1 eV beneath the conduction band edge, and are solely due to Ti atoms. More importantly, these frontier orbitals are due to edge Ti atoms specifically located at the interface between the (001) and the (101) facets; the edged Ti atoms are low-coordinated junctures between (001) and (101) surfaces.

We also find that these frontier orbital states are very localized; the number of accessible atoms, as defined by W in Ref. (19), is no more than 10 atoms. These highly localized edged Ti atoms thus are strong adsorption sites for water or other molecules. And although it is accepted that (001) facets are more active for both adsorption and dissociation and (101) facets are less so, we find that the most reactive sites for nanoparticles are actually at the interface between these two facets on these unsaturated Ti sites. These sites therefore provide unique surface structural properties in nanoparticles where a variable of facets exist.

References:

1.	Diebold U. The surface science of titanium dioxide. Surf Sci Rep. 2003;48(5-8):53-229.

2.	Diebold U, Ruzycki N, Herman GS, Selloni A. One step towards bridging the materials gap: surface studies of TiO2 anatase. Catal Today. 2003;85(2-4):93-100.

3.	Zhang HZ, Banfield JF. Thermodynamic analysis of phase stability of nanocrystalline titania. J Mater Chem. 1998;8(9):2073-6.

4.	Ranade MR, Navrotsky A, Zhang HZ, Banfield JF, Elder SH, Zaban A, et al. Energetics of nanocrystalline TiO2. P Natl Acad Sci USA. 2002;99:6476-81.

5.	d'Hennezel O, Ollis DF. Surface prechlorination of anatase TiO2 for enhanced photocatalytic oxidation of toluene and hexane. Helv Chim Acta. 2001;84(11):3511-8.

6.	Nagaveni K, Sivalingam G, Hedge MS, Madras G. Solar photocatalytic degradation of dyes: high activity of combustion synthesized nano TiO2. Appl Catal B-Environ. 2004;48(2):83-93.

7.	Gao Y, Elder SA. TEM study of TiO2 nanocrystals with different particle size and shape. Mater Lett. 2000;44(3-4):228-32.

8.	McCormick JR, Zhao B, Rykov SA, Wang H, Chen JGG. Thermal stability of flame-synthesized anatase TiO2 nanoparticles. J Phys Chem B. 2004;108(45):17398-402.

9.	Li GS, Li LP, Boerio-Goates J, Woodfield BF. High purity anatase TiO2 nanocrystals: Near room-temperature synthesis, grain growth kinetics, and surface hydration chemistry. J Am Chem Soc. 2005;127(24):8659-66.

10.	Barnard AS, Zapol P, Curtiss LA. Anatase and rutile surfaces with adsorbates representative of acidic and basic conditions. Surf Sci. 2005;582(1-3):173-88.

11.	Arrouvel C, Digne M, Breysse M, Toulhoat H, Raybaud P. Effects of morphology on surface hydroxyl concentration: a DFT comparison of anatase-TiO2 and gamma-alumina catalytic supports. J Catal. 2004;222(1):152-66.

12.	Vittadini A, Selloni A, Rotzinger FP, Gratzel M. Structure and energetics of water adsorbed at TiO2 anatase (101) and (001) surfaces. Phys Rev Lett. 1998;81(14):2954-7.

13.	Bredow T, Jug K. Sindo1 Study of Photocatalytic Formation and Reactions of Oh Radicals at Anatase Particles. J Phys Chem-Us. 1995;99(1):285-91.

14.	Ohno T, Sarukawa K, Matsumura M. Crystal faces of rutile and anatase TiO2 particles and their roles in photocatalytic reactions. New J Chem. 2002;26(9):1167-70.

15.	Gong XQ, Selloni A. Reactivity of anatase TiO2 nanoparticles: The role of the minority (001) surface. J Phys Chem B. 2005;109(42):19560-2.

16.	Gong XQ, Selloni A, Vittadini A. Density functional theory study of formic acid adsorption on anatase TiO2(001): Geometries, energetics, and effects of coverage, hydration, and reconstruction. J Phys Chem B. 2006;110(6):2804-11.

17.	Kay A, Cesar I, Gratzel M. New benchmark for water photooxidation by nanostructured alpha-Fe2O3 films. Journal of the American Chemical Society. 2006;128(49):15714-21.

18.	Yang HG, Sun CH, Qiao SZ, Zou J, Liu G, Smith SC, et al. Anatase TiO2 single crystals with a large percentage of reactive facets. Nature. 2008;453(7195):638-U4.

19.	Wang H, Lewis JP. Second-generation photocatalytic materials: anion-doped TiO2. J Phys-Condens Mat. 2006;18(2):421-34.

20.	Tully JC. Molecular Dynamics with electronic transitions. J Chem Phys. 1990;93.

21.	Hammes-Schiffer S, Tully JC. Proton-Transfer in Solution - Molecular-Dynamics with Quantum Transitions. J Chem Phys. 1994;101(6):4657-67.

22.	Doltsinis NL, Marx D. Nonadiabatic Car-Parrinello molecular dynamics. Physical Review Letters. 2002;88(16):-.

23.	Craig CF, Duncan WR, Prezhdo OV. Trajectory surface hopping in the time-dependent Kohn-Sham approach for electron-nuclear dynamics. Physical Review Letters. 2005;95(16):-.

24.	Tapavicza E, Tavernelli I, Rothlisberger U. Trajectory surface hopping within linear response time-dependent density-functional theory. Physical Review Letters. 2007;98(2):-.